## Slide 1: Towards bottom-up design of porous electrode microstructures An approach coupling evolutionary algorithms and pore network modelling Maxime van der Heijden, Rik van Gorp, Gabor Szendrei, Mohammad Amin Sadeghi, Jeffrey Gostick, Antoni Forner Cuenca
241st ECS Meeting, Vancouver, BC, Canada
June 1st, 2022

## Slide 2: Redox flow batteries for large-scale energy storage
Rechargeable
Decoupled energy (tank size) and power (reactor size): upscaling possibilities
Currently too expensive
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump

## Slide 3
Porous electrodes engineering is a multicomplex optimization problem
100
A(n-1)+  An+ + e-
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump
Key properties:
Surface area ↑
Pressure drop ↓
Mass transport ↑
Mechanical properties ↑
Electrochemical activity ↑
(Electro)chemical stability ↑

## Slide 4
Current generation not optimized, affecting three major losses:
Activation losses
Ohmic losses
Mass transport losses
Tailored electrodes for all-liquid systems
Hierarchical organization
↓ Pressure drop
↑ Electrochemical performance
200 μm

## Slide 5: Bottom-up design of porous electrodes
Experimental
characterization
Pore network
model
Genetic
optimization
Battery tests
Chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Evolution theory
Self-evolving

## Slide 6: “All models are wrong, but some are useful”
Level of complexity and detail
Lattice Boltzmann model
0.3 mm
Concentration map
Pore network model
1.0 mm
Macroscopic continuum model
[mol m-3]

## Slide 7: Pore network extraction from a commercial porous electrode
X-ray
Tomography
SNOW
Algorithm
Void
Solid
100
z
y
x
200 μm
100
Paper electrode
X-ray
Tomography
SNOW
Algorithm
z
y
x
200 μm
Cloth electrode
200

## Slide 8: Iterative pore network model
Iterative algorithm:
Fluid transport
Species transport
Charge transport
Coupled
Membrane
Current collector
Anode
Cathode
Ions
Ions
A(n-1)+
An+
A(n-1)+
An+
Load
e-
e-

## Slide 9: Network-in-series to model species depletion
Iterative algorithm:
Fluid transport
Species transport
Charge transport
Coupled
1 mm
17 mm

## Slide 10: Assessing the versatility by experimental validation
Symmetric battery design, validated for:
2 Electrodes
3 Velocities
2 Chemistries
20, 5.0, and 1.5 cm s-1
Anode
Cathode
Membrane
A(n-1)+
An+
A(n-1)+
An+
Ions
Ions
Load
Current collector
e-
Pump
e-
Fe3+
Fe2+

## Slide 11: Non-aqueous electrolytes as a model case
Cloth
Active species: 0.1 M TEMPO. / TEMPO+
Salt: 1 M TBAPF6
Solvent: Acetonitrile
Electrode: Paper

## Slide 12: Incomplete wetting of the porous structure frustrates simplified descriptions
Fe3+
Fe2+
Active species: 0.1 M Fe2+ / Fe3+
Salt: 1 M NaCl
Solvent: Water
Electrode: Paper
Pore network model: Experiment:
Mass transfer coefficient fitting:

## Slide 13: Local reactant depletion
Cloth electrode
Paper electrode
Inlet
Outlet
Concentration [mol m-3]
0 – 1 mm
16 – 17 mm
8 – 9 mm
z
x
y
x
y
z
Inlet
Outlet

## Slide 14: Bimodal pore structure for lower pressure drops
Current collector
Membrane
Cloth electrode
Paper electrode
y
x
z
 | Paper | Cloth
KIP[μm2] | 4.2 | 44
KTP [μm2] | 1.2 | 21
KIP:KTP | 3.4 | 2.1

## Slide 15: Are commercial electrodes too thick?
Cloth electrode
Paper electrode
Current
collector
Membrane
20 cm s-1
z
y
x
1.5 cm s-1
y
z
x
Membrane
168 mA cm-2
1 V: 266 mA cm-2
280 mA cm-2
232 mA cm-2

## Slide 16: Screening operation envelopes
Cloth electrode
Paper electrode
Fe3+
Fe2+
Ppump = Pel
Ppump = 0.1Pel
Ppump = Pel
Ppump = 0.1Pel

## Slide 17: Bottom-up design of porous electrodes
Experimental
characterization
Pore network
model
Genetic
optimization
Battery tests
Chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Evolution theory
Self-evolving

## Slide 18

Gene pool
Parents
Crossover
Selection
Mutation
N species
2nd generation
Termination
Selection
Criteria
Population
N species
1st generation
Generation
Evolutionary theory

## Slide 19: Proof of principle
= 50
= 10
= 1000
= [13x13x4]
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
Fitness
Pumping power, Ppump
Electrical power, Pel
+ 75% Fitness
- 72% Ppump
+ 42% Pel

## Slide 20: Structure evolution
= 50
= 10
= 1000
= [13x13x4]
Generation 0
Generation 999
0 10 20 30 40
Pore diameter [μm]
0 4 8 12 16
Throat radius [μm]
100 μm
Thickness
Membrane
Current collector
Flow direction
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
Flow direction

## Slide 21: Bottom-up design of porous electrodes
Experimental
characterization
Pore network
model
Genetic
optimization
Battery tests
Chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Evolution theory
Self-evolving

## Slide 22: The big picture
Experimental
characterization
Pore network
model
Genetic
optimization
Advanced
manufacturing
Device
implementation
+
+
+

## Slide 23: Acknowledgments
Contact:
m.v.d.heijden@tue.nl
Electrochemical Materials and Systems