## Slide 1: Stereolithography 3D Printing As a Versatile Tool to Manufacture Porous Electrodes for Redox Flow Batteries Maxime van der Heijden, Marit Kroese, Jacky Olinga, Zandrie Borneman, and Antoni Forner-Cuenca Abstract number: #L09-2889
244th ECS Meeting
October 10th, 2023

## Slide 2: Porous electrode engineering is a complex multiscale optimization problem
100
A(n-1)+  An+ + e-
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump

## Slide 3: Tailored electrodes for all-liquid systems
Current generation not optimized, affecting three major losses:
Activation losses
Ohmic losses
Mass transport losses
Hierarchical organization
↓ Pressure drop
↑ Electrochemical performance
200 μm

## Slide 4: Bottom-up design of porous electrodes
500 μm
500 μm
Experimental
characterization
Pore network
model
Genetic
optimization
Advanced
manufacturing
Device
implementation
Battery tests
Redox chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Theory of evolution
Self-evolving
3D printing
Pillar design
Carbonization
Post-treatment
Durability
Cost analysis
[1]
[3]
[4]
[2]

## Slide 5: Additive manufacturing of ordered porous carbon electrodes for redox flow batteries
Stereolithography
VRFB (0.1 M VOSO4 in 3M H2SO4):
10 mA cm-2 0.5 - 1.3 V
Direct ink writing
ilim: 1 - 50 mM ferrocyanide in 1M KCl
Wang, P. et al., Adv. Mater. Technol., 5 (5), 1901030 (2020)
1 mm
What is the impact of the electrode structure on
the mass transport properties of ordered lattice
structures in flow cells?

## Slide 6: From 3D printing plastic to conductive electrodes
Oxidation
250 °C
5 h
1 °C min-1
Carbonization
850 °C
1 h
5 °C min-1
Flow cell
testing
1 mm
1 cm
1 cm
500 μm
0.1 M TEMPO / TEMPO+ in 1 M TBAPF6 in acetonitrile

## Slide 7: Proof-of-principle stereolithography printing
Air
N2
Test
Printing platform
Liquid resin
Resin tank
UV light
Mirror
Lens
Light source
Cured model
300 μm pillars
900 x 900 x 900 μm3 pores
XY spot size 85 μm
Z resolution 25 μm
Methacrylate(s) 25-45 wt%
Acrylate(s) 45-65 wt%
Urethane Dimethacrylate 7-10 wt%
Photo initiator < 0.9 wt%

## Slide 8: Carbonization results in shrinkage
500 μm
Bottom
Top
Side
Carbonized
Oxidation T
Carbonization T
Air
N2
Test
Printed Carbonized
Porosity [%] 77 59
Internal surface area [m-1] 2700 4700-6600
Carbon content [atom%]* 77 82
Oxygen content [atom%]* 20 12
Nitrogen content [atom%]* 3 1
Conductivity [S m-1] 0 85
Oxidation: 11% isotropic shrinkage
Carbonization: 45% anisotropic shrinkage
*X-ray photoelectron spectroscopy

## Slide 9: Tweaking the carbonization process  manufacturing guidelines
3D print
Printing platform
Horizontal
Vertical
Diagonal
Platform direction
1 cm
Air
N2
Test
The printing direction impacts the electrode performance through a change in morphology, resulting in enhanced performance for diagonally printed electrodes.
Porosity
Thermal sequence
Sample holder
Printing direction vs. the printing platform
3D print porosity:
Thermal sequence:
Sample holder:
Cell architecture: 3D printed electrode, square pillars, flow-through flow field
How do the 3D printed electrodes perform
compared to commercial materials?

## Slide 10: Electrochemical and hydraulic performance of 3D printed electrodes
Cell architecture: square pillars, horizontal printing direction, flow-through flow field
3D printed, 0.70
Paper, 0.85
Cloth, 0.88
3D printed Commercial
Conductivity [S m-1] 85 122
Ohmic resistance [Ω] 1.5 0.9
Porosity [%] 59 80
Pore size distribution [μm] 490-530 2-40
Thickness [μm] 1000 210
Internal surface area [m-1] 4700-6600 72000
100
100
1000
3D print
Paper
Cloth
Pressure drop:
Mass transport:
Dimensionless:
3D printed electrodes: ↓internal surface area, ↓pressure drop, and ↑mass transfer coefficient.
How can we further enhance mass transfer
rates of 3D printed electrodes?

## Slide 11: Interaction between flow field and electrode determines reactor performance
FTFF, 0.70
IDFF, 0.65
Inlet
Outlet
Porous
electrode
Flow direction
Rib
Channel
Flow through
Interdigitated
Inlet
Outlet
Interdigitated vs. flow-through flow fields:
↑pressure drop, but also ↑mass transfer coefficient.
Desing based on reactor architecture and operating conditions
Cell architecture: 3D printed electrode, square pillars, horizontal printing direction

## Slide 12: Engineering the pillar geometry can improve mass transfer rates
Triangle, 0.74
Square, 0.70
Helix, 0.70
Triangle, 0.74
Square, 0.70
Cylinder, 0.65
Helix, 0.70
Cylinder
Square
Triangle
Helix
500 μm
Square
Square Triangle Cylinder Helix
Internal
surface area [m-1] 6600 5800 5900 7700
Exponent [-] 0.70 0.74 0.65 0.70
Helical or triangular pillar shapes enhance mass transfer rates
Cylinder, 0.65
Cylinder
Square
Triangle
Helix
2 mm

## Slide 13: 3D printing of flow battery electrodes
Proof-of-principle
Manufacturing guidelines
Porosity, thermal sequence, sample holder, printing direction vs. the printing platform
Enhanced mass transport and decreased pressure drop
Desing based on reactor architecture and operating conditions
Pillar structures promise increased mass transfer rates
Air
N2
Test
3D print
Paper
Flow through
Interdigitated
Triangle
Helix

## Slide 14: Towards next-generation flow battery electrodes
Fine-tune resin formulation and carbonization steps
Finer resolutions
Multi-scale electrode structures
Combined with topology optimizers
Goal: excellent electrochemical performance and low hydraulic resistance

## Slide 15: Acknowledgments
Contact:
m.v.d.heijden@tue.nl

## Slide 16: Cyclic voltammetry data