## Slide 1: Starting from the bottom: Coupling a genetic algorithm and a pore network model for redox flow battery porous electrode optimization Maxime van der Heijden, Rik van Gorp, Gabor Szendrei, Victor de Haas, Mohammad Amin Sadeghi, Jeffrey Gostick, and Antoni Forner Cuenca
ModVal 2023 #19, Duisburg, Germany
March 22nd, 2023
ModVal 2023 - #19

## Slide 2
Porous electrode engineering is a multicomplex optimization problem
100
A(n-1)+  An+ + e-
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump
Key properties:
Surface area ↑
Mass transport ↑
Pressure drop ↓
Mechanical properties ↑
Electrochemical activity ↑
(Electro)chemical stability ↑

## Slide 3
Current generation not optimized, affecting three major losses:
Activation losses
Ohmic losses
Mass transport losses
Tailored electrodes for all-liquid systems
Hierarchical organization
↓ Pressure drop
↑ Electrochemical performance
200 μm

## Slide 4: Bottom-up design of porous electrodes
Experimental
characterization
Pore network
model
Genetic
optimization
Advanced
manufacturing
Device
implementation
Battery tests
Chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Theory of evolution
Self-evolving
3D printing
Phase separation
Carbonization
Post-treatment
Durability
Cost analysis

## Slide 5: All models are wrong, but some are useful
Level of complexity and detail
Lattice Boltzmann model
0.3 mm
Concentration map
Pore network model
1.0 mm
Macroscopic continuum model
[mol m-3]

## Slide 6: Pore network extraction from a commercial porous electrode
X-ray
Tomography
SNOW
Algorithm
Void
Solid
100
z
y
x
200 μm
100
Paper electrode
X-ray
Tomography
SNOW
Algorithm
z
y
x
200 μm
Cloth electrode
200

## Slide 7: Iterative pore network model
Iterative algorithm:
Fluid transport
Charge transport
Species transport
Coupled
Membrane
Current collector
Anode
Cathode
Ions
Ions
A(n-1)+
An+
A(n-1)+
An+
Load
e-
e-

## Slide 8: Network-in-series to model species depletion
Iterative algorithm:
Fluid transport
Charge transport
Species transport
Coupled
1 mm
17 mm
Does this model represent reality?

## Slide 9: Assessing the versatility and robustness by experimental validation
Symmetric battery design, validated for:
2 Electrodes
3 Velocities
2 Chemistries TEMPO and Iron
20, 5.0, and 1.5 cm s-1
Anode
Cathode
Membrane
A(n-1)+
An+
A(n-1)+
An+
Ions
Ions
Load
Current collector
e-
Pump
e-
Fe3+
Fe2+

## Slide 10: Non-aqueous electrolytes as a model case
Cloth
Active species: 0.1 M TEMPO. / TEMPO+
Salt: 1 M TBAPF6
Solvent: Acetonitrile
Electrode: Paper

## Slide 11: Incomplete wetting of the porous structure frustrates simplified descriptions
Fe3+
Fe2+
Active species: 0.1 M Fe2+ / Fe3+
Salt: 1 M NaCl
Solvent: Water
Electrode: Paper
Pore network model: Experiment:
Mass transfer coefficient fitting:
This model is a simplification of reality,
so how can this model be used?

## Slide 12: Predicting profiles is the strength of pore network models
Cloth electrode
Paper electrode
z
x
y
x
y
z
Flow
direction
0 20 40 60 80 100
Concentration [mol m-3]
0 – 1 mm
1.5 cm s-1

## Slide 13: Predicting profiles is the strength of pore network models
Cloth electrode
Paper electrode
z
x
y
x
y
z
y
x
z
Flow
direction
0 20 40 60 80 100
Concentration [mol m-3]
0 5 10 15 20 25
Pressure [MPa]
103 104 105
Current [A m-3]
0 – 1 mm
1.5 cm s-1
y
z
x
Membrane

## Slide 14: Bottom-up design of porous electrodes
Experimental
characterization
Pore network
model
Genetic
optimization
Advanced
manufacturing
Device
implementation
Battery tests
Chemistries
Imaging
Network extraction
Pore simulations
Parameter analysis
Bottom-up
Theory of evolution
Self-evolving
3D printing
Phase separation
Carbonization
Post-treatment
Durability
Cost analysis

## Slide 15

Gene pool
Parents
Crossover
Selection
Mutation
N species
2nd generation
Termination
Selection
Criteria
Population
N species
1st generation
Generation
Developing a genetic algorithm using the theory of evolution
Diameter

## Slide 16: Proof of principle
= 50
= 10
= 1000
= [13x13x4]
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
Fitness
Pumping power, Ppump
Electrical power, Pel
+ 75% Fitness
- 72% Ppump
+ 42% Pel

## Slide 17: Structure evolution
= 50
= 10
= 1000
= [13x13x4]
Generation 0
Generation 999
0 10 20 30 40
Pore diameter [μm]
0 4 8 12 16
Throat radius [μm]
100 μm
Thickness
Membrane
Current collector
Flow direction
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
Can we optimize more realistic structures?

## Slide 18: The evolution of advanced network geometries
Generation 0
Generation 999
100 μm
Generation 0
Generation 499
Carbon paper
Cubic lattice
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
Cubic lattice
+ 11% Fitness
- 33% Ppump
+ 0% Pel
0 10 20 30 40
Pore diameter [μm]
SNOW
Algorithm
Flow direction

## Slide 19: Incorporating design flexibility by pore merging and splitting
Merging
Splitting
Generation 0
Generation 999
Pore diameter evolution
Generation 0
Generation 999
+ Merging and splitting
Diameter
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
0 10 20 30 40
Pore diameter [μm]
100 μm
Flow direction
+ 39% Fitness
- 56% Ppump
+ 9% Pel

## Slide 20: The influence of flow field induced flow pathways in the electrode
Flow-through flow field
Interdigitated flow field
Inlet
Outlet
Rib
x
y
z
500 μm
80
90
100
Concentration [mol m-3]
Membrane
Inlet
Outlet
Membrane
0
0.1
0.2
Absolute velocity [cm s-1]
0.05
0.15
Membrane
y
z
Outlet
Inlet
Rib
Membrane
Outlet
Inlet
Outlet
Outlet
Inlet
Inlet

## Slide 21: The influence of flow field induced flow pathways on the evolution
Generation 0
Generation 999
Flow-through flow field
Generation 0
Generation 486
Interdigitated flow field
Outlet
Inlet
Rib
Flow direction
0.2 M Vanadium, 0.5 V, 1.5 cm s-1
100 μm
0 10 20 30 40
Pore diameter [μm]
+ 88% Fitness
- 75% Ppump
+ 24% Pel

## Slide 22: The big picture
Experimental
characterization
Pore network
model
Genetic
optimization
Advanced
manufacturing
Device
implementation
+
+
+

## Slide 23: Acknowledgments
Contact:
m.v.d.heijden@tue.nl
ModVal 2023 - #19