## Slide 1: Engineering Porous Electrodes for Redox Flow Batteries Modeling, Diagnostics, and Manufacturing Maxime van der Heijden
Amcel Symposium
November 1st, 2024

## Slide 2: Urgent need for renewable technologies and energy storage at a large scale Redox flow batteries for energy storage on a daily basis
Sunrise
Midday
Sunset
Demand
Solar energy
1800
1900
2021
40
80
120
160
Year
Energy consumption x 103 [TWh]
0
Renewable energy
The Netherlands:
~100 GW renewable energy required
Todays storage: ~50 MW
Increase storage 1000x
~150 MW/month energy storage required

## Slide 3: Urgent need for renewable technologies and energy storage at a large scale Efficiency losses hamper widespread implementation
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump

## Slide 4: Urgent need for renewable technologies and energy storage at a large scale We need tailored electrode microstructures for redox flow batteries
Anode
Cathode
A(n-1)+
An+
A(n-1)+
An+
Membrane
Ions
Ions
Load
Current collector
e-
e-
Catholyte
Anolyte
Pump
Pump
A(n-1)+  An+ + e-
250 μm
250 μm
250 μm
Key properties:
- Surface area
- Permeability
- Mass transport
- Conductivity
Porous electrodes

## Slide 5: Urgent need for renewable technologies and energy storage at a large scale Engineering porous materials for electrochemical devices
Current generation not optimized, affecting three major losses:
Activation losses
Ohmic losses
Mass transport losses
Hierarchical organization
↓ Pressure drop
↑ Electrochemical performance
200 μm

## Slide 6
500 μm
Pore network
model
Genetic
optimization
Cell-level
imaging
500 μm
Additive
manufacturing
Network extraction
Pore simulations
Parameter analysis
Bottom-up design
Pore-level
Self-evolving
Operando
Neutron radiography
Redox chemistries
3D printing
Structural freedom
Carbon electrodes
Engineering porous electrodes for redox flow batteries Bottom-up design of porous electrodes

## Slide 7
All models are wrong, but some are useful
Pore-scale modeling
Level of complexity and detail
Lattice Boltzmann model
0.3 mm
Concentration map
Pore network model
1.0 mm
Macroscopic continuum model
[mol m-3]

## Slide 8
Assessing the versatility of pore network models
Pore network models connect microstructural effects with resulting battery performance
Network
extraction
Void
Solid
Iterative algorithm:
1. Fluid transport
2. Species transport
3. Charge transport
Organic electrolyte:
Aqueous electrolyte:

## Slide 9
Assessing the versatility of pore network models
Pore network models connect microstructural effects with resulting battery performance
Network
extraction
Void
Solid
Iterative algorithm:
1. Fluid transport
2. Species transport
3. Charge transport
0 100
Concentration [mol m-3]
Thickness [-]
Length [-]
Current [-]
250 μm
Flow direction
103 105
Current [A m-3]
Current profile:
Concentration profile:

## Slide 10
The influence of the flow field and electrode thickness
Co-design of electrode and flow field geometry is necessary for efficient system operation

## Slide 11
500 μm
Pore network
model
Genetic
optimization
Cell-level
imaging
500 μm
Additive
manufacturing
Network extraction
Pore simulations
Parameter analysis
Bottom-up design
Pore-level
Self-evolving
Operando
Neutron radiography
Redox chemistries
3D printing
Structural freedom
Carbon electrodes
Engineering porous electrodes for redox flow batteries Bottom-up design of porous electrodes

## Slide 12: Genetic optimization of electrode structures Bimodal pore size distribution enhances the performance
Increased fitness:
↑ Electrochemical power
↓ Pumping power
Genes
Generation
Selection
Crossover
Mutation
Selection
Generation
Termination
Fitness
Generation
Pumping power
Generation
Electrical power
Generation
How does the optimized electrode look like?

## Slide 13: Genetic optimization of electrode structures Bimodal pore size distribution enhances the performance
Increased fitness:
↑ Electrochemical power
↓ Pumping power
Genes
Generation
Selection
Crossover
Mutation
Selection
Generation
Termination
100 μm
Flow direction
0 10 20 30 40
Pore diameter [μm]
1000 generations
Thickness
Membrane
Current collector
Can we optimize more realistic structures?

## Slide 14: Towards realistic battery operation Unique electrode structures are needed for a given reactor design and operating conditions
Membrane
An+
A(n-1)+
e-
e-
An+
A(n-1)+
Load
Anode
Cathode
Flow-through Interdigitated
Chemistry
Microstructural freedom:
Diameter
change
Merging and
splitting
Random
Ordered
VO2+
VO2+
e-
e-
Reactor parameters:
Flow field

## Slide 15: Towards realistic battery operation Enhancing the performance of conventional electrode designs
100 μm
0 10 20 30 40
Pore diameter [μm]
z
y
x
100 μm
Generation 1
1000 generations
Generation 1000
Flow direction
Cubic electrode
Conventional electrode
Vanadium electrolyte:
v = 1.5 cm s-1

## Slide 16: The effect of the electrolyte chemistry on the electrode optimization The trade-off between electrochemically active surface area and through-plane conductivity
100 μm
100 μm
Generation 1000
Flow direction
Cubic electrode
Conventional
Vanadium electrolyte
TEMPO electrolyte
v = 1.5 cm s-1

## Slide 17
500 μm
Pore network
model
Genetic
optimization
Cell-level
imaging
500 μm
Additive
manufacturing
Network extraction
Pore simulations
Parameter analysis
Bottom-up design
Pore-level
Self-evolving
Operando
Neutron radiography
Redox chemistries
3D printing
Structural freedom
Carbon electrodes
Engineering porous electrodes for redox flow batteries Bottom-up design of porous electrodes

## Slide 18
Novel operando neutron radiography approach
Concentration profiles under a voltage bias can be visualized
+
-
Detector
Neutron beam
Tank 1
Tank 2
Reactor
+
-
Cumulative concentration
0.0 M
1.0 M

## Slide 19
Novel operando neutron radiography approach
Concentration profiles under a voltage bias can be visualized
[BF4-]
0.0 M
0.5 M
Flight tube
Neutron
beam
MCP Detector
Chopper
Time of Flight
based energy
separation
Reactor
Pulsed
beam
Supporting electrolyte concentration

## Slide 20
500 μm
Pore network
model
Genetic
optimization
Cell-level
imaging
500 μm
Additive
manufacturing
Network extraction
Pore simulations
Parameter analysis
Bottom-up design
Pore-level
Self-evolving
Operando
Neutron radiography
Redox chemistries
3D printing
Structural freedom
Carbon electrodes
Engineering porous electrodes for redox flow batteries Bottom-up design of porous electrodes

## Slide 21
From 3D printing plastic to conductive electrodes
Customized and tunable 3D printed electrodes can be manufactured
Printing platform
Liquid resin
Resin tank
UV light
Mirror
Lens
Light source
Cured
model
1 cm
Oxidation
Carbonization
Flow cell testing

## Slide 22
From 3D printing plastic to conductive electrodes
Customized and tunable 3D printed electrodes can be manufactured
Pillar structures
Cylinder
Square
Triangle
Helix
2 mm
100
100
1000
3D print
Paper
Cloth
Compared to commercial electrodes
1 cm
Oxidation
Carbonization
Flow cell testing

## Slide 23
Engineering porous electrodes for redox flow batteries
Additive manufacturing of porous electrodes
100 μm
Metal
3D printing
Metal electrodes
Stereolithography
Reduction
Topology
optimization
Cell-level
imaging
Bottom-up design
Flow fields
Continuum
Operando
Confocal imaging
Cell design
Additive
manufacturing
Structural freedom
Carbon electrodes
Advanced designs
500 μm

## Slide 24: Next step - Engineering porous electrodes for redox flow batteries Additive manufacturing of porous electrodes
Advanced designs - TPMS
1 cm
Oxidation
Carbonization
Flow cell testing
Pillar design impacts mass transport
Cylinder
Square
Triangle
Helix
2 mm
Primitive
Gyroid
IWP
Diamond
1 mm
Cubic
lattice

## Slide 25
e-
Multiphase mass transport
Advanced manufacturing
Component optimization
Platform
Tank
Light source
Flooding
Multi-layers
Integrated
Manufacturing techniques
Materials engineering
–
Structure design
Surface chemistry
Electrochemical devices
Microreactors
–
Imaging approaches
Computational fluid dynamics
Reactor design and operation
conditions dependent optimized
transport layers
–
Computational optimization
Layer integration
25
January 1st – Assistant Professor at the University of Waterloo, Canada
Advanced Manufacturing of Electrochemical Devices

## Slide 26: Acknowledgments
Antoni Forner-Cuenca, Rik van Gorp, Vanesa Muñoz Perales (UC3M), Rémy Jacquemond, and Emre Burak Boz
Gabor Szendrei, Victor de Haas, Marit Kroese, Jacky Olinga, Mojtaba Barzegari, Zandrie Borneman, and the rest of EMS
UW: Jeff Gostick, Mohammad Amin Sadeghi
PSI: Pierre Boillat, Eric Ricardo Carreon Ruiz
MIT: Fikile Brushett, Kevin Tenny, Katharine Greco
Contact:
m.v.d.heijden@tue.nl
maximeheijden@outlook.nl
https://maximevdheijden.github.io/
Till December 31st: Starting January 2025: